## Slide 1
KTK mould Nr. | WZ-1274
Customer mould Nr. | 2025-142
Valid CAD file | NB5 Y light cover FL_12792-759_20251023 + NB5 Y light cover RR_12792-758_20251023
Part name | Y Housing NB5 FL Y Housing NB5 FR
Part number | 12792-758 12792-759
Material | PP-TD 20
Color | Pls provide
Shrinkage flow direction | 1.013， pls confirm
Shrinkage cross direction | 1.013， pls confirm
Surface cavity | 2+2
12792-759
12792-758

## Slide 2
2. Parting Line / main demolding direction
3. Gate Locates
4. Ejection
8. Finish Require
1. Assembly situation
13. Proposals / part optimization
Content / mould
6. Mould body size / check with mould spec
12. Important measurements based on 2D
5. insert
9. Draft angle
10. Wall thickness
11. Engraving
7. Additional mould proposal
Content / part

## Slide 3
1. Assembly situation
12792-759
12792-758

## Slide 4
2. Parting lines / main demolding direction
Cavity
Core

## Slide 5
2. Parting lines / main demolding direction
12792-759
12792-758

## Slide 6
3. Gate locations
进胶点处做一个Φ4*0.3深凹点辅助进胶，后模加凸起。请确认？
Cut Φ4*0.3 on cavity side and add material on core side acc. , pls confirm
每个产品一点尖点进胶
Mold Masters one tip for each part
后模加凸起
Core side

## Slide 7
4. Ejection
具体以3D为准
Ejector pin 顶针
12792-759
12792-758

## Slide 8
6. Mould body size check with mould spec
GB
GB
GB
GB
GB
GB
GB
GB
码模板尺寸500m
码模板尺寸450mm
TOP
DATUM
SR:请提供
Pls provide SR info.
ARBURG
470 C 1500-350

## Slide 9
8. Finish requirements
12792-759
12792-758

## Slide 10
9. Draft angle
Core：后模
Cavity ：前模
12792-759
12792-758

## Slide 11
10. Wall thickness
深红色区域成型后会有缩水印，
为防止产品表面有缩水风险，建议调整肉厚。
carmine area with sink mark risk, is it OK?
12792-758

## Slide 12
10. Wall thickness
12792-759
深红色区域成型后会有缩水印，
为防止产品表面有缩水风险，建议调整肉厚。
carmine area with sink mark risk, is it OK?

## Slide 13
11. Engraving
产品空间位置不够，放不下日期章/年章，能不能只刻字？请确认？
Not have a suitable area put month&year date insert,
can we just make resin marking and cav NO. as show?

## Slide 14
12. Important measurement based on 2D

## Slide 15
13. Proposals / part optimization
箭头指示蓝色区域为倒扣，需要优化改至出前模。
Undercut, can you improve the 3D to cancel it?
12792-758
箭头指示红色区域为倒扣，需要改至出后模。
Red area with Undercut, can you improve the 3D
to cancel it?

## Slide 16
12792-759
产品红色区域分型面需要优化改至出前模。
Suggest chang red area to cavity side
13. Proposals / part optimization

## Slide 17
12792-759
产品蓝色区域为倒扣，需要优化改至出后模。
Blue area with undercut, can you improve the part 3D?
13. Proposals / part optimization

## Slide 18
13. Proposals / part optimization
模肉
cavity
模胚
Mold base
此温度感应器HY找不到资料和购买方，请是否可以如上图一样在模具中加上图中的孔即可，请确认，多谢！
This temp. sensor not available to buy it here, can we just make a hole in the mold acc. To above dimension?