## Slide 1
Revision 01
for project: part name: CARRIER_NB5_MIKO
Used plastic material: A5132T-TD PP+TD20
Used CAD File name:13077-655.stp/23.10.25 03:14

## Slide 2
Molding Material
Material Introduction
1. Melt Density 0.89677 g/cm^3
2. Solid Density 1.0817 g/cm^3
3. Ejection Temperature 120 °c
4. Recommended Mold Temperature 40 °c
5. Recommended Melt Temperature 220 °c
6. Absolute Max. Melt Temperature 270°c
7. Melt Temperature Minimum 190 °c
8. Melt Temperature Maximum 230 °c
9. Mold Temperature Minimum 30°c
10. Mold Temperature Maximum 60°c
11. Maximum Shear Rate 100000.00 1/s
12. Maximum Shear Stress 0.25 MPa
A5132T-TD PP+20%TD
Viscosity model
PVT profile

## Slide 3
Molding Material
Material Introduction
A5132T-TD PP+20%TD

## Slide 4
Molding setting parameters
(Filling Conditions)
(Mold temperature ):
(Cavity) 40 C
(Core) 40 C
(See the analysis results of cooling)
(Melt temperature): 220.0 C
(Injection time): 0.5S
(Filling and Packing curve)
保压曲线(Packing curve)

## Slide 5
Molding setting parameters
Process Setup
Part Details and Tool Description
Part Name: | CARRIER_NB5_MIKO
Part Volume | 47.84 cm^3
Nominal Wall Thickness | 1.8 mm
Tool Description | 1*4cavities
Material | A5132T-TD PP+20%TD
Injection time | 0.6138 s
Material temp | 220[deg.c]
Mold temp | 40 [deg.c]
Velocity/Pressure Transfer (% volume) | 98 %
Packing Pressure | 80+50% filling pressure / 5+5s
Project Area | 133.28 m^2
Part、Tool、Setup

## Slide 6
Molding setting runner system
Ø hot runner
Ø runner
Ø injection point
Hot runner with tip-gate
The hot gate:Ø1.5
The hot runner:Ø10mm
G1(-100,-128.4)
G2(-27.9,-126.9)
G3(-100,107.8)
G4(-27.9,109.3)
G5(27.9,126.9)
G6(100,128.4)
G8(27.9,-109.3)
G7(100,-107.8)

## Slide 7
Content FILL+PACK (minimum)
1. Fill time SHADED
2. Fill time CONTOUR
3. Pressure X/Y plot
4. Pressure at V/P switchover
5. Temperature at flow front
6. Temperature / Bulk temperature
7. Volumetric shrinkage
8. Time to reach ejection temperature
9. Frozen layer fraction
10. Clamp force XY plot
11. Share rate and stress
12. Sink mark depth (mm)
13. Air traps
14. Weld lines

## Slide 8
Fill Time
The flow is balance , and no short shot occur on this condition.

## Slide 9
The flow is balance , and no short shot occur on this condition.
Fill Time

## Slide 10
The flow is balance , and no short shot occur on this condition.
Fill Time

## Slide 11
The flow is balance , and no short shot occur on this condition.
Fill Time

## Slide 12
(Fill time )(sec) | 0.6138 | (Whether there is clear hesitation) | No
Fill time- contour

## Slide 13
Fill Time (Animation)
Play Shift + F5 show flow animation

## Slide 14
Play Shift + F5 show flow animation
Fill Time (Animation)

## Slide 15
Pressure X/Y plot

## Slide 16
V/P Pressure
The max injection pressure at sprue : 27.43Mpa
The maximum injection pressure is reasonable

## Slide 17
Flow Front temperature
The result shows the temperature of the polymer when the flow front reached a specified node.
The melt temperature : 220℃
Max melt temperature in part : 221.6℃
Min melt temperature in part : 210.2℃
The temperature difference : 11.4℃

## Slide 18
Flow Front temperature
The result shows the temperature of the polymer when the flow front reached a specified node.
The melt temperature : 220℃
Max melt temperature in part : 221.6℃
Min melt temperature in part : 210.2℃
The temperature difference : 11.4℃

## Slide 19
Temperature / Bulk temperature

## Slide 20
The shrinkage at ejection is not very evenly on the part surface.
Volumetric Shrinkage

## Slide 21
The shrinkage at ejection is not very evenly on the part surface.
Volumetric Shrinkage

## Slide 22
Time to reach ejection temperature

## Slide 23
Frozen layer fraction

## Slide 24
Clamp force XY plot
The clamp force request is 25tonne.

## Slide 25
11. Share rate and stress

## Slide 26
11. Share rate and stress

## Slide 27
Sink mark depth (mm)
There is a risk of shrinkage marks in the area around the red wire frame.

## Slide 28
Air Traps
There is NO air traps on the part surface.

## Slide 29
There is NO air traps on the part surface.
Air Traps

## Slide 30
Weld Lines
There is weld line on the hole edges of the part surface.

## Slide 31
There is weld line on the hole edges of the part surface.
Weld Lines

## Slide 32
Content WARP
15. Deflection all effects
16. Deflection all effects X
17. Deflection all effects Y
18. Deflection all effects Z
19. Shrinkage compensation
Content cooling
20. Circuit coolant temperature
21. Circuit flow rate
22. Circuit Reynolds number
23. Circuit metal temperature
24. Time to reach ejection temp. / part
25. Frozen layer percentage
26. Circuit heat removal efficiency
27. Temperature mould / part

## Slide 33
the distribution of overall warpage for the different area of the part surface
The over all deformation is 0.58mm（include shrinkage).

## Slide 34
the distribution of overall warpage for the different area of the part surface
The over all deformation is 0.58mm（include shrinkage).

## Slide 35
Max. deflection on the X direction
The maximum deflection value is -0.43~0.50 mm on the X direction .

## Slide 36
Max. deflection on the Y direction
The maximum deflection value is -0.19~0.19mm on the Y direction .

## Slide 37
Max. deflection on the Z direction
The maximum deflection value is -0.10~0.29mm on the Z direction .

## Slide 38
Dynamic process for the overall warpage value
Press « shift+F5 » and look at this slide to see the animated ，Press 《Esc 》to end.

## Slide 39
Circuit coolant temperature
无

## Slide 40
Circuit flow rate
无

## Slide 41
Circuit Reynolds number
无

## Slide 42
Circuit metal temperature
无

## Slide 43
Time to reach ejection temp. / part
无

## Slide 44
Circuit heat removal efficiency
无

## Slide 45
Temperature, part
mold temperature is 60 ℃ .
The recommend T-mold range is 25.0℃ ~107.6℃;
the mold temperature is reasonable. Cooling sys is suitable on the surface.
无

## Slide 46
Temperature, part
mold temperature is 60 ℃ .
The recommend T-mold range is 25.0℃ ~107.6℃;
the mold temperature is reasonable. Cooling sys is suitable on the surface.
无

## Slide 47
The result indicate
1.The filling is evenly ,and no short shot of the picture shown gates position.
2.The injection pressure is 27.43Mpa, the pressure in the acceptable range .
3. The difference of temperature front temp is less than 20℃ .
4. There is air traps on the ribs of the part surface.
5. There is weld line on the hole edge of the part surface.
6.Volumetric shrinkage is not evenly on the part surface.
7. The total deflection is 0.58mm.
Analysis result as below
fill time | inject pressure | Max. clamp | Warpage X direction | Warpage Y direction | Warpage Z direction
0.6138Sec | 27.43Mpa | 25 tonne | -0.43~0.50mm | -0.19~0.19mm | -0.10~0.29mm
MFR Summary + conclusion