## Slide 1
KTK mould Nr. | WZ-1275
Customer mould Nr. | 25.009
Valid CAD file | Y Housing NB5 RL_12792-760.stp+Y Housing NB5 RR_12792-761.stp
Part name | Y Housing NB5 RL Y Housing NB5 RR
Part number | 12792-760 12792-761
Material | PP-TD 20
Color | Pls provide
Shrinkage flow direction | 1.2%
Shrinkage cross direction | 1.2%
Surface cavity | 2+2
12792-760
12792-761
12792-761
12792-760

## Slide 2
2. Parting Line / main demolding direction
3. Gate Locates
4. Ejection
8. Finish Require
1. Assembly situation
13. Proposals / part optimization
Content / mould
6. Mould body size / check with mould spec
12. Important measurements based on 2D
5. insert
9. Draft angle
10. Wall thickness
11. Engraving
7. Additional mould proposal
Content / part

## Slide 3
1. Assembly situation
12792-760
12792-761
12792-760
12792-761

## Slide 4
2. Parting lines / main demolding direction
Cavity
Core
Core
Cavity

## Slide 5
2. Parting lines / main demolding direction
12792-760
12792-761
12792-760
12792-761

## Slide 6
3. Gate locations
尖点进胶
Tip gate
进胶点处做一个Φ4*0.3深凹点辅助进胶，后模加凸起。请确认？
Cut Φ4*0.3 on cavity side and add material on core side acc. , pls confirm
后模加凸起
Core side

## Slide 7
4. Ejection
具体以3D为准
Ø4 Ejector pin Ø4顶针
Ø6 Ejector pin Ø6顶针
Ø3 Ejector pin Ø3顶针
Ø3 Ejector pin
先预留位置，T1后有需要再加
Ø3 Ejector pin will add after T1 if needed

## Slide 8
6. Mould body size check with mould spec
GB
GB
GB
GB
GB
GB
GB
GB
clamp plate:550m
TOP
DATUM
clamp plate:450m'm
mold thickness: 501mm
470
470
550
定位环：φ125
Location ring: φ125
SR: flat

## Slide 9
8. Finish requirements

## Slide 10
9. Draft angle
Core：后模
Cavity ：前模
建议后模骨位绿色面朝后模方向做3°的出模角度
Suggest add 3°draft angel, pls check improved part 3D and confirm it
此绿色建议朝前模方向做3°的出模角度
Suggest add 3°draft angel, pls check improved part 3D and confirm it

## Slide 11
10. Wall thickness
深红色区域成型后会有缩水印，
为防止产品表面有缩水风险，建议调整肉厚。
carmine area with sink mark risk, is it OK?

## Slide 12
11. Engraving
Pls check part 3D and confirm if it’s OK for
>engraving info.
>engraving location
>engraving size
Material and cav NO.
part no.
date stamps
month & year
revision grid

## Slide 13
12. Important measurement based on 2D

## Slide 14
13. Proposals / part optimization
模肉
模胚
此温度感应器HY找不到资料和购买方，请是否可以如上图一样在模具中加上图中的孔即可，请确认，多谢！
This temp. sensor not available to buy it here, can we just make a hole in the mold acc. To above dimension?

## Slide 15
13. Proposals / part optimization
箭头指示蓝色区域为倒扣，需要优化改至出前模。
Undercut , need change to cavity side, pls check modified part 3D and confirm it

## Slide 16
Y Housing NB5 RL_12792-760与Y Housing NB5 RR_12792-761是镜像件，我司只提供一个产品的DFM
Y Housing NB5 RL_12792-760 and Y Housing NB5 RR_12792-761 are symmetrical
Pls check both improved part 3D(modified areas colored red)) and give your feedback & confirmation